Refined Methodology Paper

Effect of Graphene Defects on Lithium Diffusion at a Silicon-Graphene Composite Anode Interface

Molecular Dynamics Project Plan - Literature Anchors, Chosen Inputs, and Discovery Outputs

| Item | Description |
| --- | --- |
| Project type | Computational molecular dynamics study |
| Primary comparison | Model A: Si slab + pristine graphene + Li vs. Model B: Si slab + vacancy-defective graphene + Li |
| Optional extension | Model C: Si slab + DV5-8-5 graphene + Li |
| Main output | Li mean squared displacement (MSD), diffusion coefficient, and defect/pristine diffusion ratio |
| Current status | Phase 1 complete; Phase 2 structure generation/visualization in progress |
| Important rule | Literature values are used as justified setup inputs; diffusion coefficients and fitting windows are discovered from this project. |

Revision purpose: This refined version separates literature-backed input values from values that must be discovered by the project. Values taken from papers are listed with specific references. Values not yet tested remain marked as pending. Version 3 update: the uploaded PDFs were cross-checked; Gao et al. journal metadata was corrected, verified 2025 Si et al. values were inserted, and the ReaxFF timestep note was updated to include 0.5 fs MD and 0.1 fs tracer-diffusion precedent.

# Abstract

This methodology paper defines a staged molecular dynamics workflow for studying lithium mobility at simplified silicon-graphene composite anode interfaces. The core comparison is between a pristine graphene interface and a vacancy-defective graphene interface while keeping the silicon slab, lithium loading, boundary conditions, force field, thermostat, and analysis workflow consistent. The main quantitative outputs will be the lithium mean squared displacement (MSD), the diffusion coefficient estimated from the linear MSD regime, and the ratio of defective-interface to pristine-interface diffusivity. This revision makes a strict distinction between literature-backed setup choices and values that must be generated or discovered by the present simulations. Literature sources support the use of Si-graphene or Si-C interface models, vacancy-type graphene defects, Li-Si-C ReaxFF as the production-force-field candidate, NVT molecular dynamics with femtosecond timesteps, elevated-temperature accelerated diffusion tests, and MSD-based diffusion analysis. Final claims must remain comparative because short high-temperature atomistic simulations do not directly predict room-temperature battery-cell performance.

# Keywords

lithium diffusion; silicon anode; graphene defect; molecular dynamics; ReaxFF; LAMMPS; mean squared displacement; Si-C composite

# 1. Research Objective and Scope

Research question: How do graphene vacancy defects affect lithium diffusion in a simplified silicon-graphene composite anode interface model?

Working hypothesis: vacancy-defective graphene may increase lithium mobility by creating voids, channels, or penetration pathways at the Si-graphene interface. The methodology also checks whether a defect improves transport at the cost of structural stability.

The project does not model a full battery cell. It isolates an atomistic interface and compares relative Li mobility trends under a common MD protocol. Electrolyte, binder, SEI formation, current collectors, electrochemical cycling, and full electrode microstructure are outside the current scope.

| Model | Structure | Purpose | Status |
| --- | --- | --- | --- |
| Phase 2 test | Graphene + Li | Validate structure generation and visualization | Current |
| Model A | Si slab + pristine graphene + Li | Baseline interface | Planned |
| Model B | Si slab + single-vacancy graphene + Li | Primary defect comparison | Planned |
| Model C | Si slab + DV5-8-5 graphene + Li | Optional publication-level extension | Optional |

# 2. Value Provenance: What Comes from Literature vs. What the Project Discovers

The table below is the central control table for this methodology. It prevents accidental mixing of literature inputs with project results.

| Parameter | Category | Chosen/planned value | Reference basis | Status |
| --- | --- | --- | --- | --- |
| Main comparison | Chosen project design supported by literature | Model A vs. Model B: pristine graphene interface vs. single-vacancy graphene interface | Current project scope; direct finite-temperature pristine/SV/DV5-8-5 comparison from Si et al. [9]; defect rationale from Qin et al. [2] | Locked for minimum project |
| Optional defect | Literature-backed extension | DV5-8-5 graphene defect | Qin et al. identified DV5-8-5 as a structurally balanced defect option; Si et al. directly compared Si/DV5-8-5 with Si/p-Gr and Si/SV [2,9] | Optional Model C |
| Force field | Literature-backed input | Li-Si-C ReaxFF from Olou'ou Guifo et al. 2023 | Developed for Si-C anode chemistry including Li, Si, sp2-C, SiC, and interfaces [4] | Exact parameter file/source still must be recorded |
| Ensemble | Literature-backed input | NVT for equilibration and production diffusion tests | Used in Chou and Hwang [1], Gao et al. [3], and Lashani Zand et al. [5] | Candidate final choice |
| Temperature | Literature-backed candidate | 800 K and/or 1200 K accelerated tests | Chou and Hwang used 800 K; Gao, Lashani Zand, and Si et al. used 1200 K [1,3,5,9] | Choose after stability tests |
| Timestep | Literature-backed candidate + stability test | Start ReaxFF testing at 0.5 fs; test 0.25, 0.5, and 1.0 fs if needed; do not copy the 3 fs AIMD timestep directly into ReaxFF | 1 fs used in Chou, Gao, and Lashani Zand; Si et al. used 3 fs AIMD; Olou'ou Guifo used 0.5 fs ReaxFF MD and 0.1 fs for tracer diffusion [1,3,4,5,9] | Final stable value discovered by short runs |
| Graphene lattice | Literature-backed reference | 2.467 A graphene lattice constant; experimental value ~2.46 A | Chou and Hwang [1] | ASE value should be checked/documented |
| Si/graphene starting separation | Literature-backed starting geometry | Approx. 2 A initial separation before relaxation | Chou and Hwang placed a-LixSi and graphene approx. 2 A apart before relaxation [1] | Final spacing discovered after minimization |
| Slab/vacuum | Literature-backed starting geometry | 18-20 A vacuum if periodic z is retained for slab tests | Qin et al. used 20 A for graphene and 18 A for Gr/Si [2] | Final box checked in OVITO/minimization |
| MSD method | Literature-backed analysis | Fit the linear MSD regime; use 3D, 2D in-plane, or direction-resolved MSD as appropriate | Chou and Hwang used n=6 for 3D and n=4 for 2D diffusion; LAMMPS compute msd reports dx2, dy2, dz2, and total MSD [1,8] | Fitting window discovered from project data |
| Diffusion coefficients | Project-discovered result | Project results: D_A, D_B, D_B/D_A, and uncertainty; literature comparators include Si et al. 2025 values for Si/p-Gr, Si/SV, and Si/DV5-8-5 | Your final values come from this project; Si et al. reports 1.88e-4, 2.32e-4, and 2.47e-4 cm2/s at 1200 K for Si/p-Gr, Si/SV, and Si/DV5-8-5 [9] | Pending |

# 3. Literature-Backed Methodological Inputs

This section lists exact values verified from the literature and how they will be used. These values are not project discoveries; they are setup anchors or justification points.

| Reference | Role | Verified values | How used in this project |
| --- | --- | --- | --- |
| Chou & Hwang 2013 | Si-graphene interface baseline | Graphene lattice constant 2.467 A; 48-C rectangular graphene sheet of 12.8187 x 9.8680 A2; a-LixSi/graphene placed approx. 2 A apart before relaxation; 500 K anneal for 1 ps; 1 fs timestep; 18 ps AIMD at 800 K; Nose-Hoover thermostat; 3 samples; D_Li near graphene = (4.74 +/- 0.60)e-5 cm2/s vs bulk a-Li1.0Si = (1.02 +/- 0.40)e-5 cm2/s; Li motion near graphene was mainly 2D/interface-parallel. | Use as the main Si-graphene interface precedent; motivates checking in-plane vs z-direction MSD. |
| Qin et al. 2021 | Defect model and slab geometry precedent | 6 x 6 graphene supercell; defect set p-Gr, SV, DV5-8-5, DV555-777; 4 x 4 Si(111) slab with two double atomic layers; bottom dangling bonds passivated with H; bottom H and Si fixed; Si-Si adjusted approx. 4% for mismatch; vacuum 20 A for graphene and 18 A for Gr/Si. DV5-8-5 monolayer barrier = 1.406 eV, ~6.153 eV lower than p-Gr. SV/Si barrier = 0.587 eV but caused strong deformation. DV5-8-5/Si was judged more structurally balanced. | Use for defect selection and optional Model C; use Si(111) if matching the defect-benchmark geometry. |
| Gao et al. 2021 | Si/C AIMD protocol and MSD fitting precedent | NVT at 1200 K; 1 fs timestep; Nose-Hoover thermostat; geometry relaxation to force <0.01 eV/A and energy change <1e-4 eV/atom; 25 ps mixture-mode and 60 ps core-shell AIMD; C layer thicknesses 2, 3, and 4 A; MSD fits selected after mixing: t >14 ps for mixture and t >45 ps for core-shell, with noisy final points omitted. D_bulk c-Si = 7.75e-5 cm2/s; Si/C mixture values = 2.097e-4, 2.028e-4, 2.003e-4 cm2/s for 2, 3, 4 A layers. | Use as a protocol anchor for high-temperature accelerated diffusion and fitting-window justification. |
| Olou'ou Guifo et al. 2023 | Production force-field candidate | J. Phys. Chem. C 127(6), 2818-2834; DOI 10.1021/acs.jpcc.2c07773. The paper reports a Li-Si-C ReaxFF parameterization for Si-C composite anodes, including Si, graphitic/sp2 carbon, SiC, interfacial motifs, lithiation, and swelling behavior. Its ReaxFF-MD applications used a 0.5 fs Verlet timestep for trajectories and 0.1 fs for tracer diffusion coefficient calculations. | Use as primary production ReaxFF candidate; record exact parameter file and atom mapping before Phase 3. Use 0.5 fs as the first ReaxFF timestep test, and reduce toward 0.1 fs if tracer diffusion or energy stability requires it. |
| Lashani Zand et al. 2023 | High-temperature NVT/MSD comparator | NVT AIMD at 1200 K, 1 fs timestep, Nose-Hoover thermostat. MSD linear fitting between 15 and 22 ps to avoid initial transients. D at 1200 K: pristine Si(100) 7.82e-5, Si/C(100) 1.57e-4, Si/C3N4(100) 3.17e-4 cm2/s; similar values reported for Si(110) and Si(111). | Use as an additional Si/C interface comparator and a clear example of explicit MSD fitting-window reporting. |
| LAMMPS documentation | Implementation constraint | pair_style reaxff requires atom_style with per-atom charges and, by default, a charge-equilibration fix such as fix qeq/reaxff. fix qeq/reaxff example uses Nevery=1, cutoffs 0.0 and 10.0, tolerance 1.0e-6. compute msd outputs dx2, dy2, dz2, and total MSD; the MSD slope is proportional to diffusion coefficient. | Use for LAMMPS input-script requirements and analysis implementation. |
| Si et al. 2025 | Direct defective-graphene AIMD comparator | Studied Si/p-Gr, Si/SV, and Si/DV5-8-5 on Si(111). Unit cells were 6.59 x 6.59 A with 30 Si and 30 Li; C counts were 14, 13, and 12 for p-Gr, SV, and DV5-8-5. The Si substrate had 10 layers; Gr-Si gap = 1.5 A; vacuum = 14 A; optimization used force <0.02 eV/A and energy change <1e-5 eV; k-grid = 3 x 3 x 1; NVT AIMD at 1200 K with a 3 fs timestep and Nose-Hoover thermostat; AIMD length = 30 ps; MSD fit used t > 15 ps; D_Li values were 1.88e-4, 2.32e-4, and 2.47e-4 cm2/s for Si/p-Gr, Si/SV, and Si/DV5-8-5. | Use as the closest literature comparator for final trend discussion and as an optional geometry benchmark. Do not copy the 3 fs timestep into ReaxFF without stability validation. |

Audit update: The 2025 ACS Omega defective-graphene paper has now been checked directly. Its numerical setup values and diffusion coefficients are included as literature comparators. They are not project results; this project must still generate its own D_A, D_B, fitting windows, and uncertainty under the chosen LAMMPS/ReaxFF protocol.

# 4. Project Phases and Repository Workflow

The project is managed as validation gates. A phase is complete only when expected files are produced, visual checks pass in OVITO, and results are committed to GitHub.

| Phase | Objective | Main folders | Pass condition | Literature use |
| --- | --- | --- | --- | --- |
| 1 | LAMMPS + OVITO validation | lammps_inputs/, trajectories/, figures/ | Trajectory opens and animates in OVITO | Low |
| 2 | Graphene + Li initial structure | structures/, figures/, notes/ | Graphene and Li geometry looks correct; no obvious overlaps | Low-moderate |
| 3 | Force-field selection/test | force_fields/, lammps_inputs/ | Li-Si-C ReaxFF loads; QEq runs; no immediate instability | High |
| 4 | Pristine Si-graphene-Li model | structures/, lammps_inputs/ | Model A minimizes and equilibrates | High |
| 5 | Defective Si-graphene-Li model | structures/, lammps_inputs/ | Model B is comparable to Model A except for vacancy | High |
| 6 | Production MD | trajectories/, logs/ | Stable trajectories with usable MSD growth | High |
| 7 | MSD and diffusion analysis | analysis/, figures/ | MSD curves, D values, fitting windows, and uncertainty | High |

## 4.1 Phase-Specific Parameter Matrix

The table below converts the seven-phase workflow into an execution matrix. It lists the parameters that must be supplied in each phase, separates literature-backed anchors from project-controlled choices, and identifies what each phase is expected to discover or validate. This table should be updated after each phase is completed.

| Phase | Required inputs | Literature-backed anchors / credible sources | Project-discovered output or pass condition |
| --- | --- | --- | --- |
| 1. LAMMPS + OVITO validation | LAMMPS executable, simple input script, dump frequency, trajectory file, OVITO visualization. | No chemistry literature required. This phase validates the software pipeline only. | LAMMPS produces a log and dump file; OVITO opens and animates the trajectory. Phase 1 screenshot is saved. |
| 2. Graphene + Li initial structure | Graphene lattice, test sheet size, Li count, Li starting height, z-vacuum, export formats. | Graphene lattice constant 2.467 A from Chou & Hwang [1]. Approximate Li-graphene starting distance near 2.3 A from Chou & Hwang [1]. Isolated graphene vacuum around 20 A from Qin et al. [2]. | Structure opens in OVITO; Li atoms are above graphene; no obvious overlaps. Exact Phase 2 sheet size and Li count remain documented project choices. |
| 3. Force-field selection and ReaxFF test | Li-Si-C ReaxFF parameter file, atom order, pair_coeff mapping, atom_style charge, QEq settings, timestep tests. | Li-Si-C ReaxFF from Olou'ou Guifo et al. [4]. Their ReaxFF-MD used 0.5 fs and 0.1 fs for tracer diffusion; LAMMPS ReaxFF/QEq requirements from LAMMPS docs [6,7]. | Correct atom mapping; QEq runs without unresolved warnings; stable short test. Final stable timestep is discovered by testing 0.25, 0.5, and/or 1.0 fs. |
| 4. Model A: pristine Si-graphene-Li | Si slab orientation, slab size, graphene sheet, Li loading, starting interface spacing, boundary conditions, minimization settings. | Qin et al. provide a Gr/Si defect-benchmark geometry using Si(111), 4 x 4 slab, and 18 A vacuum [2]. Si et al. provide a smaller AIMD geometry: Si(111), 10 layers, 6.59 x 6.59 A, 30 Si, 14 C, 30 Li [9]. | Minimized and equilibrated pristine interface. Final atom counts, relaxed interface spacing, and stable Model A geometry are project outputs. |
| 5. Model B: vacancy-defective Si-graphene-Li | Same inputs as Model A plus vacancy construction: removed C atom, defect position, and identical Li loading/box/protocol. | SV and DV5-8-5 are supported by Qin et al. [2]. Si et al. directly compared Si/p-Gr, Si/SV, and Si/DV5-8-5 and found higher D_Li in the defective systems [9]. | Model B differs from Model A only by the vacancy; it minimizes and equilibrates without collapse. Defect-induced structural changes are observed. |
| 6. Production MD | Chosen temperature, timestep, thermostat damping, equilibration length, production length, dump frequency, random seeds. | NVT is supported by Chou, Gao, Lashani Zand, and Si et al. [1,3,5,9]. Literature temperatures include 800 K and 1200 K; production examples include 18, 25, 30, and 60 ps depending on model type. | Stable trajectories for Model A and Model B. Final temperature, timestep, equilibration length, and production length are confirmed by stability and MSD quality. |
| 7. MSD and diffusion analysis | MSD dimensionality, coordinate unwrapping, fitting-window rule, unit conversion, repeats/statistics, output plots. | Chou demonstrates 2D/interface-parallel diffusion treatment; Gao and Si et al. use MSD linear fitting after mixing; Si et al. fit t > 15 ps for Si/Gr composites [1,3,9]. | Li MSD curves, D_A, D_B, D_B/D_A, direction-resolved MSD, fitting windows, and uncertainty. These are project results, not literature inputs. |

Interpretation rule: values in the literature-backed column justify starting choices. Values in the project-discovered column must not be filled in until the relevant simulation or analysis phase has passed its validation checks.

## 4.2 Repository structure

Li_Diffusion_Si_Graphene/
  literature/        literature review, primary-source notes, references
  force_fields/      ReaxFF parameter files and source notes
  structures/        ASE builders and LAMMPS data/XYZ files
  lammps_inputs/     input scripts for validation, minimization, equilibration, production
  trajectories/      dump files and run outputs
  logs/              LAMMPS log files and copied run summaries
  analysis/          Python scripts for logs, MSD, fitting, plots
  figures/           OVITO screenshots and final plots
  docs/              workflow documentation
  notes/             phase validation notes

# 5. Atomic Model Construction

Atomic structures will be generated with scripted Python/ASE workflows. Manual edits are avoided unless they are documented in notes and reproducible scripts.

| Parameter | Refined method choice | Literature anchor | Project action |
| --- | --- | --- | --- |
| Graphene lattice constant | Use ASE default, record actual value; literature reference 2.467 A | Chou & Hwang [1] | Confirm generated C-C bonds and box dimensions |
| Phase 2 graphene size | Use a small test sheet; 48-C sheet is a literature precedent, but Phase 2 may use any clearly documented test size | Chou & Hwang [1] | Visual validation only; not final science model |
| Li starting height over graphene | Initial placement can use approx. 2.3 A as a literature-informed starting distance; avoid overlaps | Chou & Hwang reported average Li-Gr distance around 2.3 A near interface [1] | Final Li positions after minimization are discovered |
| Si slab orientation | Recommended first publication-style choice: Si(111), because the defect benchmark uses Gr/Si on Si(111) | Qin et al. [2] | If Si(100) is chosen instead, justify as a separate design choice |
| Si slab size | Use a model commensurate with graphene; literature precedent is 4 x 4 Si(111) with two double atomic layers | Qin et al. [2] | Final size depends on LAMMPS cost and matching |
| Graphene-Si separation | Start at approx. 2 A before relaxation or use relaxed spacing from structure builder | Chou & Hwang [1] | Final spacing after minimization is project-generated |
| Vacuum / z dimension | Use at least 18 A slab vacuum for initial periodic-z tests; 20 A for isolated graphene tests | Qin et al. [2] | May be adjusted based on boundary conditions |
| Defect construction | Remove one central C atom for SV; keep all other variables identical to Model A | Qin et al. [2] | Record removed atom ID/index and defect coordinates |
| DV5-8-5 optional model | Construct only after Model A and B pass; use established topology | Qin et al. [2] | Optional extension |
| Direct Si/Gr AIMD benchmark geometry | Optional geometry anchor: Si(111), 10-layer substrate, 6.59 x 6.59 A cell, 30 Si and 30 Li; p-Gr/SV/DV5-8-5 C counts = 14/13/12; initial Gr-Si gap = 1.5 A; 14 A vacuum. | Si et al. [9] | Use only if choosing to closely benchmark the 2025 AIMD study; otherwise use as a comparator and document deviations. |

# 6. Force-Field Strategy

The final systems require Li-Li, Si-Si, C-C, Li-Si, Li-C, and Si-C interactions. The production force field must therefore be a ternary Li-Si-C potential rather than an unsupported mixture of unrelated subsystem potentials.

| Force-field option | Role | Required documentation | Status |
| --- | --- | --- | --- |
| Li-Si-C ReaxFF from Olou'ou Guifo et al. 2023 | Primary production candidate | Exact file name; source DOI or repository; atom order; pair_coeff mapping; any control file; version/date | Literature-supported; file pending |
| Li/C ReaxFF | Auxiliary carbon-side check only | File/source if used; not valid for full Si-containing interface | Optional |
| Li/Si force field | Auxiliary pure-silicon check only | File/source if used; not valid for full C-containing interface | Optional |

LAMMPS ReaxFF requirement: Use atom_style charge or an equivalent per-atom charge property. With pair_style reaxff, LAMMPS expects charge equilibration by default; the Phase 3 input script should include a qeq/reaxff-type fix unless there is a documented reason not to use it.

# 7. Molecular Dynamics Protocol

Production MD begins only after structure validation and ReaxFF validation. The sequence is energy minimization, NVT equilibration, then production NVT dynamics. Model A and Model B must use the same protocol.

| Stage | Purpose | Acceptance check | Failure response |
| --- | --- | --- | --- |
| Energy minimization | Remove bad contacts and relax initial geometry | Energy decreases; no atom collapse; reasonable final interface spacing | Fix overlaps, spacing, atom types, boundaries |
| Short ReaxFF/QEq test | Check force-field loading and charge equilibration | No immediate crash; charge values finite; no atom explosion | Correct atom mapping, qeq settings, timestep |
| NVT equilibration | Bring model to chosen temperature | Temperature fluctuates around target; structure remains interpretable | Reduce timestep; adjust thermostat damping |
| Production NVT | Collect trajectory for Li diffusion | Trajectory stable; Li MSD shows analyzable growth | Extend run, repeat, or adjust simulation conditions |

| MD parameter | Refined candidate value | Literature basis | Finalization rule |
| --- | --- | --- | --- |
| Ensemble | NVT | Used in Chou & Hwang, Gao et al., and Lashani Zand et al. [1,3,5] | Use for Model A and B unless a documented issue occurs |
| Temperature | Main accelerated test: choose 800 K or 1200 K; optional lower-temperature check later | 800 K in Chou & Hwang; 1200 K in Gao, Lashani Zand, and Si et al. [1,3,5,9] | Choose after ReaxFF stability tests; report as comparative |
| Timestep | Start ReaxFF tests at 0.5 fs; test 0.25, 0.5, and 1.0 fs if needed; reduce toward 0.1 fs for tracer-diffusion-quality checks if necessary | 1 fs AIMD precedent [1,3,5]; Si et al. used 3 fs AIMD [9]; Olou'ou Guifo used 0.5 fs ReaxFF MD and 0.1 fs for tracer diffusion [4]. ReaxFF stability must be tested directly. | Largest stable timestep with acceptable energy/temperature behavior |
| Thermostat | Nose-Hoover style NVT in LAMMPS | Nose-Hoover used in reviewed AIMD studies [1,3,5] | Set damping in input script and validate temperature behavior |
| Equilibration | Minimum explicit equilibration before measuring MSD; use ps-scale tests | 500 K 1 ps anneal in Chou; full-mixing/fitting windows in Gao and Si et al. [1,3,9] | Do not start MSD until temperature and structure are stable |
| Production length | Initial test: short; final target: tens of ps or longer if feasible | 18 ps in Chou; 25/60 ps in Gao; 25 ps with 15-22 ps fit in Lashani Zand; 30 ps in Si et al. [1,3,5,9] | Extend until MSD has a defensible linear region |
| Charge equilibration | fix qeq/reaxff every 1 step as first test; tolerance 1e-6 is a documented LAMMPS example | LAMMPS qeq/reaxff docs [7] | Record final command and convergence behavior |

# 8. Diffusion Analysis

The primary quantitative metric is lithium MSD. The analysis should use unwrapped coordinates or LAMMPS compute msd so that periodic-boundary crossings are treated correctly.

MSD(t) = < | r_i(t) - r_i(0) |^2 >

D = (1 / 2d) * d(MSD)/dt, where d is the diffusion dimensionality. For 3D diffusion, D = slope/6. For 2D in-plane diffusion, D = slope/4. For 1D direction-resolved diffusion, D = slope/2.

| Analysis output | Source | Purpose | Acceptance rule |
| --- | --- | --- | --- |
| Temperature vs time | LAMMPS log | Thermostat stability | No runaway heating/cooling; fluctuations centered near target |
| Energy vs time | LAMMPS log | Detect blow-up or bad geometry | No unphysical divergence during production |
| 3D Li MSD | compute msd or trajectory analysis | Overall Li mobility | Linear window identified and same method applied to A/B |
| In-plane MSD (x-y) | Trajectory post-processing or c_msd[1]+c_msd[2] | Interface-parallel motion | Reported because Si-graphene interfaces can be anisotropic |
| z-direction MSD | Trajectory post-processing or c_msd[3] | Penetration/interface-normal motion | Reported if Li crosses graphene/interface |
| Diffusion coefficient | Linear fit to MSD | Main result | Fit window, units, and regression method documented |
| Uncertainty | Independent repeats | Reliability of trend | At least 3 seeds per model if feasible |
| OVITO snapshots | Dump trajectory | Mechanistic interpretation | Show Li pathways/trapping without overclaiming |

Fitting-window rule: Do not choose the MSD fitting window before seeing this project's data. The window is a project-discovered value. Literature examples: Chou disregarded the first few picoseconds; Gao fitted after full mixing using t > 14 ps for mixture mode and t > 45 ps for core-shell mode; Lashani Zand fitted 15-22 ps; Si et al. fitted t > 15 ps for Si/p-Gr, Si/SV, and Si/DV5-8-5.

# 9. Data Generated by This Project and Discoveries Expected

| Generated data | Generated from | Discovery enabled |
| --- | --- | --- |
| Minimized Model A and Model B structures | LAMMPS minimization | Whether both models are physically stable and comparable |
| Equilibrated structures | NVT equilibration | Whether temperature and geometry remain stable |
| Li trajectories | Production dump files | Whether Li moves along graphene, through the defect, into Si, or becomes trapped |
| Li MSD curves | LAMMPS compute or Python trajectory analysis | Relative mobility in pristine vs defective interfaces |
| D_A and D_B | Linear MSD fitting | Whether the vacancy increases or decreases Li diffusion |
| D_B/D_A ratio | Diffusion coefficient comparison | Magnitude of defect effect under the chosen protocol |
| Direction-resolved MSD | x, y, z displacement analysis | Whether motion is in-plane or interface-normal |
| Repeat-run statistics | Different random seeds | Uncertainty and reliability of the trend |

# 10. Validation and Sanity Checks

| Validation level | Question | Evidence | Pass condition |
| --- | --- | --- | --- |
| Software | Do LAMMPS and OVITO work? | Phase 1 log, trajectory, screenshot | Trajectory opens and plays in OVITO |
| Structure | Is the model reasonable? | Atom counts, minimum distances, OVITO view | No overlaps; Li placement plausible; box/vacuum reasonable |
| Force field | Does Li-Si-C ReaxFF load correctly? | Short run log and charges | No immediate crash; finite charges; correct atom mapping |
| QEq | Does charge equilibration behave? | QEq output and absence of max-iteration warnings | QEq converges or warnings are documented and fixed |
| MD stability | Does the system stay physical? | Temperature/energy plots and OVITO trajectory | No atom explosion or unphysical collapse |
| Analysis | Is diffusion extracted consistently? | MSD scripts and fitting window notes | Same method for Model A and Model B |
| Literature | Are claims defensible? | Comparison to references [1-5] | Final claim remains comparative |

# 11. Limitations and Risk Controls

| Risk | Why it matters | Control |
| --- | --- | --- |
| Unvalidated force field | Can create misleading diffusion trends | Use Li-Si-C ReaxFF; document source and mapping; run subsystem sanity checks |
| Too-short trajectory | MSD may not reach a linear regime | Extend production; report fitting window; do repeat runs |
| High-temperature overinterpretation | 800-1200 K results are not room-temperature battery predictions | State that conclusions are comparative under the chosen MD protocol |
| Defect concentration artifact | Small cells exaggerate vacancy concentration | Document cell size; keep Model A/B dimensions consistent; do larger-cell check if possible |
| Anisotropic diffusion | 3D MSD can hide interface-parallel motion | Report in-plane and z components when possible |
| Single-run noise | Diffusion coefficients fluctuate | Run independent seeds and report uncertainty |
| Unverified literature numbers | Incorrect values weaken the methods section | Only use values directly verified from primary sources; mark unknowns pending |

# 12. Expected Deliverables

Phase 1 LAMMPS + OVITO validation screenshot.

Phase 2 graphene + Li structure-generation script and OVITO screenshot.

Force-field source note with exact Li-Si-C ReaxFF file name and atom mapping.

LAMMPS data files for Model A and Model B.

Minimization, equilibration, and production LAMMPS input scripts.

Temperature and energy stability plots.

Li MSD curves for pristine and defective models.

Diffusion coefficients with fitting-window documentation and unit conversion.

Repeat-run uncertainty if feasible.

OVITO snapshots showing Li motion/pathways.

Final report or manuscript-style paper with limitations and literature comparison.

# 13. Planned Final Claim Format

A suitable final claim will be:

This study compares relative lithium diffusion behavior in simplified pristine and vacancy-defective Si-graphene interface models under a common molecular dynamics protocol. The results indicate whether graphene vacancy defects increase, decrease, or do not significantly change Li mobility within the limits of the chosen Li-Si-C ReaxFF force field, model size, temperature, and simulation length.

Claim boundary: Do not claim that the model proves improved real battery performance. Experimental cell testing and longer multiscale modeling would be required for that claim.

# References

[1] Chou, C.-Y.; Hwang, G. S. Role of Interface in the Lithiation of Silicon-Graphene Composites: A First Principles Study. Journal of Physical Chemistry C 2013, 117, 9598-9604. DOI: 10.1021/jp402368k.

[2] Qin, S.; et al. Lithium Diffusion in Silicon Encapsulated with Graphene. Nanomaterials 2021, 11, 3397. DOI: 10.3390/nano11123397.

[3] Gao, X.; Lu, W.; Xu, J. Insights into the Li Diffusion Mechanism in Si/C Composite Anodes for Lithium-Ion Batteries. ACS Applied Materials & Interfaces 2021, 13, 21362-21370. DOI: 10.1021/acsami.1c03366.

[4] Olou'ou Guifo, S. B.; Mueller, J. E.; van Duin, D.; Talkhoncheh, M. K.; van Duin, A. C. T.; Henriques, D.; Markus, T. Development and Validation of a ReaxFF Reactive Force Field for Modeling Silicon-Carbon Composite Anode Materials in Lithium-Ion Batteries. Journal of Physical Chemistry C 2023, 127(6), 2818-2834. DOI: 10.1021/acs.jpcc.2c07773.

[5] Lashani Zand, A.; et al. Comprehensive Study of Lithium Diffusion in Si/C-Layer and Si/CN Composite Anodes. ACS Omega 2023, 8, 44698-44707. DOI: 10.1021/acsomega.3c05523.

[6] LAMMPS Documentation. pair_style reaxff command. https://docs.lammps.org/pair_reaxff.html.

[7] LAMMPS Documentation. fix qeq/reaxff command. https://docs.lammps.org/fix_qeq_reaxff.html.

[8] LAMMPS Documentation. compute msd command. https://docs.lammps.org/compute_msd.html.

[9] Si, L.; Huang, R.; Liu, F.; Chen, Q.; Ouyang, P.; Dou, Z. Study on the Influence of Defective Graphene on the Li Diffusion Performance in Si/Defective Graphene Composite Anodes: an Ab Initio Molecular Dynamics Study. ACS Omega 2025, 10, 19502-19509. DOI: 10.1021/acsomega.4c11709.

Revision note: This document intentionally marks untested project-specific values as pending. Final values should be filled in only after the corresponding validation phase passes.